|  | Pneumatická magnetická tyč - N42SH-Ø65 mm - SFH-2" Číslo výrobku: E0020042 |
| --- | --- |

Vlastnosti

| Popis | Pneumatická magnetická tyč - N42SH-Ø65 mm - SFH-2" |
| --- | --- |
| Číslo výrobku | E0020042 |
| Produktový klíč | SFH-S-2"-01R-HT MAGNET BAR |
| Product name | Magnetic insert for SFH-2" |
| Suitable for food production | Yes |
| Max. particle size | 10 mm |
| Min. Fe-particle size that can be caught | 0,03 mm |
| Production stop required during ferrous particles disposal | Yes |
| Cleaning (ferrous particles disposal) method | Automatic |
| Ferrous particles disposal via | Clean In Place (CIP) / Steam In Place (SIP) |
| Pneumatic connection | For 6 mm hose |
| Materials in contact with product | AISI316L (SS 1.4404) |
| Surface finishing (interior/exterior) | S5: Vibratory polished, Ra 0,4 µm, ex. welds and end faces |
| Welds inside the product channel | WM: Continuously welded |
| Welds outside the product channel | WM: Continuously welded |
| Magnetic system | 1 Magnetic bar, CIP-type |
| Magnet quality | Neodymium N-42SH |
| Magnetic bars position / behaviour during production | Static, fixed position |
| Magnetic bar size | Tube Ø65 mm |
| Number of magnetic bars | 1 |
| Flux density on magnet tube in contact with product (±10%) | 11300 gauss |
| Pneumatic supply magnetic bars | 4 (recommended) - 6 (max.) bar |
| Diameter | Ø130 mm |
| Height | 249 mm |
| Weight | 5,4 kg |