|  | Magnetické jednotky - 3xN52-Ø52,4 mm - SECE3030 Číslo výrobku: E0066661 |
| --- | --- |

Vlastnosti

| Popis | Magnetické jednotky - 3xN52-Ø52,4 mm - SECE3030 |
| --- | --- |
| Číslo výrobku | E0066661 |
| Produktový klíč | SECE-S-3030-MAGNET INSERT ASSY |
| Product name | Magnetic insert for SECE-3030 |
| Suitable for food production | For non-perishable foods only |
| Max. particle size | 10 mm |
| Min. Fe-particle size that can be caught | 0,03 mm |
| Materials in contact with product | AISI304 (SS 1.4301) / AISI316L (SS 1.4404) |
| Surface finishing (interior/exterior) | S1: Grit blasted, Ra 3 µm |
| Welds inside the product channel | WM: Continuously welded |
| Welds outside the product channel | WM: Continuously welded |
| Magnetic system | Magnetic bar in tube |
| Magnet quality | Neodymium N-52 |
| Magnetic bars position / behaviour during production | Static, fixed position 1 row |
| Magnetic bar size | Ø52,4 mm (wall thickness 1,2 mm) |
| Number of magnetic bars | 3 |
| Flux density on magnet tube in contact with product (±10%) | 12000 gauss |
| Pneumatic supply magnetic bars | 4 - 6 bar |
| Length | 866 mm |
| Width | 538 mm |
| Height | 118 mm |
| Weight | 28 kg |