|  | Magnetická vložka - 7xN42SH-Ø23 mm - SFND-DN100 Číslo výrobku: M39883 |
| --- | --- |

Vlastnosti

| Popis | Magnetická vložka - 7xN42SH-Ø23 mm - SFND-DN100 |
| --- | --- |
| Číslo výrobku | M39883 |
| Produktový klíč | SFND-S-100 INSERT NdFeB HT |
| Product name | Magnetic insert for Magnetic filter SFND-100 |
| Max. particle size | 16 mm |
| Min. Fe-particle size that can be caught | 0,03 mm |
| Production stop required during ferrous particles disposal | Yes |
| Cleaning (ferrous particles disposal) method | Manual |
| Ferrous particles disposal via | Manually taking out magnets + pulling them out of extractor |
| Materials in contact with product | AISI316L (SS 1.4404) |
| Surface finishing (interior/exterior) | S1: Grit blasted, Ra 3 µm |
| Welds inside the product channel | Wm: Continuously welded |
| Welds outside the product channel | Wm: Continuously welded where possible |
| Max. operating temperature | 140 °C |
| Min./max. ambient temperature | -20 to 60 °C |
| Max. operating pressure (pipeline pressure) | 10 bar |
| Test pressure | 15 bar |
| Magnetic system | Magnetic bar in extractor tube |
| Magnet quality | Neodymium N-42SH |
| Magnetic bars position / behaviour during production | Static, fixed position |
| Magnetic bar size | Extractor tube Ø25 mm; magnetic bar Ø23 mm |
| Number of magnetic bars | 7 |
| Flux density on (internal) magnetic bar (±10%) | 10700 gauss |
| Flux density on magnet tube in contact with product (±10%) | 8000 gauss |
| Length | 296 mm |
| Width | 220 mm |
| Height | 204.5 mm |
| Weight | 9.9 kg |