|  | Magnetrotor - 5xN45SH-Ø30 mm - SECR2020 Artikel Nummer: E0153206 |
| --- | --- |

Eigenschaften

| Beschreibung | Magnetrotor - 5xN45SH-Ø30 mm - SECR2020 |
| --- | --- |
| Artikel Nummer | E0153206 |
| Produktschlüssel | SECR-S-2020-05C-HT-B ROTOR |
| Product name | Rotor for Rotating cleanflow-2020 |
| Suitable for food production | Yes |
| Max. particle size | 10 mm |
| Ferrous particles disposal via | Manually taking out magnets + pulling them out of extractor |
| Materials in contact with product | AISI316 (SS 1.4401) / AISI316L (SS 1.4404) |
| Surface finishing (interior/exterior) | S5: Vibratory polished, Ra 0,4 µm, ex. welds and end faces |
| Extra wear-resistant coating | No |
| Welds inside the product channel | Wm: Continuously welded |
| Max. operating temperature | 100 °C |
| Min./max. ambient temperature | -20 to 40 °C |
| Magnetic system | Magnetic bar in extractor tube |
| Magnet quality | Neodymium N-45SH |
| Magnetic bars position / behaviour during production | Rotating, magnetic bars placed in a rotor |
| Magnetic bar size | Extractor tube Ø32 mm; magnetic bar Ø30 mm |
| Number of magnetic bars | 5 |
| Flux density on (internal) magnetic bar (±10%) | 13000 gauss |
| Flux density on magnet tube in contact with product (±10%) | 10500 gauss |
| Length | 198 mm |
| Width | 160 mm |
| Height | 160 mm |
| Weight | 7,7 kg |