|  | Magnetgitter - #250 mm Artikel Nummer: SEMR252538 |
| --- | --- |

Eigenschaften

| Beschreibung | Magnetgitter - #250 mm |
| --- | --- |
| Artikel Nummer | SEMR252538 |
| Produktschlüssel | SMR-N-0250x250x40-05E-S6-B |
| Shape | Square |
| Size | 250x250 mm |
| Max. particle size | 10 mm |
| Min. Fe-particle size that can be caught | 0,03 mm |
| Cleaning (ferrous particles disposal) method | Manual |
| Ferrous particles disposal via | Manually taking out magnets + pulling them out of extractor |
| Materials in contact with product | AISI316L (SS 1.4404) |
| Surface treatment/finishing | S1: Grit blasted, Ra 3 µm |
| Welds | WM: continuously welded |
| Extractor tubes brazed in housing | No |
| Max. operating temperature | 60 °C |
| Min./max. ambient temperature | -20 to 60 °C |
| ATEX marking | Free of own ignition sources |
| Suited for use in ATEX zone | 20, 21 and 22 |
| Waterproof | Yes |
| Magnetic system | Magnetic bar in extractor tube |
| Magnet quality | Neodymium N-42 |
| Magnetic bar size | Extractor tube Ø25 mm; magnetic bar Ø23 mm |
| Number of magnetic bars | 5 |
| Flux density on (internal) magnetic bar (±10%) | 10700 gauss |
| Flux density on magnet tube in contact with product (±10%) | 8000 gauss |
| Length | 250 mm |
| Width | 250 mm |
| Height | 40 mm |
| Weight | 6,2 kg |