|  | Plattenmagnet – Neodym - 200 mm Artikel Nummer: SVMN060200 |
| --- | --- |

Eigenschaften

| Beschreibung | Plattenmagnet – Neodym - 200 mm |
| --- | --- |
| Artikel Nummer | SVMN060200 |
| Produktschlüssel | SVM-N-114x34-0200-B-F1M |
| Min. Fe-particle size that can be caught | 0,03 mm |
| Advised max. installation height | 65-80 mm |
| Production stop required during ferrous particles disposal | Yes |
| Cleaning (ferrous particles disposal) method | Manual |
| Ferrous particles disposal via | Manually by wiping |
| Installation/transport interface | Threaded hole M8 (2x) |
| Material housing | AISI316L (SS 1.4404) |
| Surface treatment/finishing | S1: Grit blasted, Ra 3 µm |
| Welds | WM: continuously welded |
| Max. operating temperature | 60 °C |
| Min./max. ambient temperature | -20 to 60 °C |
| Magnetic system | Permanent Neoflux™ magnet |
| Magnet quality | Neodymium N-35 |
| Magnet field strength (flux density) (±10%) | 4000 gauss |
| Incl. cleaning tray | No |
| Length | 200 mm |
| Width | 114 mm |
| Height | 34 mm |
| Weight | 5,3 kg |