|  | Neodymium - NdFeB stock magnet - Block Article number: E0132972 |
| --- | --- |

Attributes

| Description | Neodymium - NdFeB stock magnet - Block |
| --- | --- |
| Article number | E0132972 |
| Product key | M-B-N48-B1-18x8x3-NN |
| Shape | Block |
| Surface treatment/finishing | NiCuNi plated |
| Max. operating temperature | 80 °C |
| Magnet quality | Neodymium N-48 |
| Min. Br value | 1370 mT |
| Min. HcB value | 836 kA/m |
| Min. HcJ value | 955 kA/m |
| Min. BH value | 358 kJ/m³ |
| Number of pole pairs | 1 |
| Magnetization direction | Through the height |
| North pole marking | Red dot |
| Density | 7,5 g/cm³ |
| Length | 18 mm |
| Width | 8 mm |
| Height | 3 mm |
| Weight | 0,00324 kg |