|  | Pot magnet - cylindrical - Ø6 mm Article number: GM16101 |
| --- | --- |

Attributes

| Description | Pot magnet - cylindrical - Ø6 mm |
| --- | --- |
| Article number | GM16101 |
| Product key | PM-BM-A-SG-D6x20 |
| Max. holding force | 2 N |
| Mounting interface | Press fit |
| Material housing | Galvanized steel |
| Max. operating temperature | 450 °C |
| Magnet quality | AlNiCo |
| Dimension magnet surface | Ø6 mm |
| Height | 20 mm |
| Weight | 0,0045 kg |