|  | Pot magnet - flat - Ø63 mm Article number: GM16409 |
| --- | --- |

Attributes

| Description | Pot magnet - flat - Ø63 mm |
| --- | --- |
| Article number | GM16409 |
| Product key | PM-BA-F-SG-D63x14 |
| Max. holding force | 350 N |
| Material housing | Galvanized steel |
| Max. operating temperature | 200 °C |
| Magnet quality | Ferrite |
| Dimension magnet surface | Ø63 mm |
| Height | 14 mm |
| Weight | 0,226 kg |