|  | Pot magnet with threaded bush - Ø10 mm Article number: GM16501 |
| --- | --- |

Attributes

| Description | Pot magnet with threaded bush - Ø10 mm |
| --- | --- |
| Article number | GM16501 |
| Product key | PM-TB-F-SG-D10x4.5x11.5xM3 |
| Max. holding force | 4 N |
| Mounting interface | Threaded hole M3 |
| Material housing | Galvanized steel |
| Max. operating temperature | 200 °C |
| Magnet quality | Ferrite |
| Dimension magnet surface | Ø10 mm |
| Height | 11,5 mm |
| Weight | 0,003 kg |