|  | Pot magnet with threaded bush - Ø40 mm Article number: GM16507 |
| --- | --- |

Attributes

| Description | Pot magnet with threaded bush - Ø40 mm |
| --- | --- |
| Article number | GM16507 |
| Product key | PM-TB-F-SG-D40x8x18xM5 |
| Max. holding force | 125 N |
| Mounting interface | Threaded hole M5 |
| Material housing | Galvanized steel |
| Max. operating temperature | 200 °C |
| Magnet quality | Ferrite |
| Dimension magnet surface | Ø40 mm |
| Height | 18 mm |
| Weight | 0,057 kg |