|  | Pot magnet with cylinder hole - ferrite Article number: GM16610 |
| --- | --- |

Attributes

| Description | Pot magnet with cylinder hole - ferrite |
| --- | --- |
| Article number | GM16610 |
| Product key | PM-HB-F-SG-D57x11xd6.5/24 |
| Max. holding force | 230 N |
| Mounting interface | Counterbore Ø6,5 mm |
| Material housing | Galvanized steel |
| Max. operating temperature | 200 °C |
| Magnet quality | Ferrite |
| Dimension magnet surface | 57 mm |
| Height | 11 mm |
| Weight | 0,13 kg |