|  | Pot magnet - flat - Ø8 mm Article number: GM17102 |
| --- | --- |

Attributes

| Description | Pot magnet - flat - Ø8 mm |
| --- | --- |
| Article number | GM17102 |
| Product key | PM-BA-S-SG-D8x4.5 |
| Max. holding force | 11 N |
| Material housing | Galvanized steel |
| Max. operating temperature | 200 °C |
| Magnet quality | Samarium-Cobalt (SmCo) |
| Dimension magnet surface | Ø8 mm |
| Height | 4,5 mm |
| Weight | 0,002 kg |