|  | Pot magnet - flat - Ø32 mm Article number: GM17108 |
| --- | --- |

Attributes

| Description | Pot magnet - flat - Ø32 mm |
| --- | --- |
| Article number | GM17108 |
| Product key | PM-BA-S-SG-D32x7 |
| Max. holding force | 220 N |
| Material housing | Galvanized steel |
| Max. operating temperature | 200 °C |
| Magnet quality | Samarium-Cobalt (SmCo) |
| Dimension magnet surface | Ø32 mm |
| Height | 7 mm |