|  | Pot magnet - flat - Ø10 mm Article number: GM17403 |
| --- | --- |

Attributes

| Description | Pot magnet - flat - Ø10 mm |
| --- | --- |
| Article number | GM17403 |
| Product key | PM-BA-N-SG-D10x4.5 |
| Max. holding force | 25 N |
| Material housing | Galvanized steel |
| Max. operating temperature | 80 °C |
| Magnet quality | Neodymium (NdFeB) |
| Dimension magnet surface | Ø10 mm |
| Height | 4,5 mm |
| Weight | 0,0025 kg |