|  | Pot magnet - rubber coated - with internal thread Article number: GM17472 |
| --- | --- |

Attributes

| Description | Pot magnet - rubber coated - with internal thread |
| --- | --- |
| Article number | GM17472 |
| Product key | PM-RTI-N-RB-70x50x13x2M5 |
| Max. holding force | 290 N |
| Shear force | 90 N |
| Mounting interface | Threaded hole M5 |
| Colour | Black |
| Max. operating temperature | 80 °C |
| Magnet quality | Neodymium (NdFeB) |
| Dimension magnet surface | 70x50 mm |
| Height | 13 mm |
| Weight | 0,149 kg |