|  | Pot magnet - rubber coated - with threaded end Article number: GM17484 |
| --- | --- |

Attributes

| Description | Pot magnet - rubber coated - with threaded end |
| --- | --- |
| Article number | GM17484 |
| Product key | PM-RTE-N-RB-D31x6xM6x17 |
| Max. holding force | 89 N |
| Shear force | 35 N |
| Mounting interface | Threaded end M6 |
| Colour | Black |
| Max. operating temperature | 60 °C |
| Magnet quality | Neodymium (NdFeB) |
| Dimension magnet surface | Ø31 mm |
| Height | 17 mm |
| Thickness | 6 mm |
| Weight | 0,024 kg |