|  | Pot magnet - rubber coated - with cylinder hole Article number: GM17557 |
| --- | --- |

Attributes

| Description | Pot magnet - rubber coated - with cylinder hole |
| --- | --- |
| Article number | GM17557 |
| Product key | PM-RHC-N-RB-D57x7.6xd8/25 |
| Max. holding force | 175 N |
| Shear force | 55 N |
| Mounting interface | Counterbore Ø8 mm |
| Colour | Black |
| Max. operating temperature | 60 °C |
| Magnet quality | Neodymium (NdFeB) |
| Dimension magnet surface | Ø57 mm |
| Height | 7,6 mm |
| Weight | 0,077 kg |