|  | Pot magnet with threaded bush - neodymium Article number: GM17603 |
| --- | --- |

Attributes

| Description | Pot magnet with threaded bush - neodymium |
| --- | --- |
| Article number | GM17603 |
| Product key | PM-TB-N-SG-D13x4.5x11.5xM3 |
| Max. holding force | 60 N |
| Mounting interface | Threaded hole M3 |
| Material housing | Galvanized steel |
| Max. operating temperature | 80 °C |
| Magnet quality | Neodymium (NdFeB) |
| Dimension magnet surface | Ø13 mm |
| Height | 11,5 mm |
| Weight | 0,005 kg |