|  | Extractor 5 bars - SFND-DN050/065 Article number: M21761 |
| --- | --- |

Attributes

| Description | Extractor 5 bars - SFND-DN050/065 |
| --- | --- |
| Article number | M21761 |
| Product key | SFND-S-EXTRACTOR DN50/DN65 |
| Product name | Extractor for Magnetic filter SFND-050/065 |
| Materials in contact with product | AISI316L (SS 1.4404) |
| Surface finishing (interior/exterior) | S3: Pickled and passivated, Ra 0,8 µm |
| Welds | WM: continuously welded |
| Tube diameter | 25 mm |
| Number of tubes | 5 |
| Length | 244 mm |
| Width | 174 mm |
| Height | 128 mm |
| Weight | 3 kg |