|  | Add-on magnetic head pulley - 650 mm Article number: RHAN22065000 |
| --- | --- |

Attributes

| Description | Add-on magnetic head pulley - 650 mm |
| --- | --- |
| Article number | RHAN22065000 |
| Product key | RHP-B219A06-065-RSD-BA |
| Shaft type | Replaceable |
| Max. particle size | 80 mm |
| Min. Fe-particle size that can be caught | 0,5 mm |
| Ferrous particles disposal method | Automatic - continuous |
| Magnetic field depth | 100 mm |
| Suitable for belt width | 650 mm |
| Roller width | 700 mm |
| Interface/connection | Shaft Ø50h7 (2x) (for SKF SNL 511-609) for SEW SA67 |
| Max. operating temperature | 60 °C |
| Min./max. ambient temperature | -20 to 40 °C |
| Magnet width | 585 mm |
| Magnetic system | Permanent Neoflux® magnet |
| Magnetic layout | Axial pole with 6 poles |
| Magnet quality | Neodymium N-38 |
| Magnet field strength (flux density) (±10%) | 3000 gauss |
| Motor drive | Not included |
| Diameter | 219 mm |
| Length | 1060 mm |
| Weight | 98 kg |