|  | Magnetic bar N42-Ø23 mm - 305 mm Article number: SBAME100000-305 |
| --- | --- |

Attributes

| Description | Magnetic bar N42-Ø23 mm - 305 mm |
| --- | --- |
| Article number | SBAME100000-305 |
| Product key | BAR-N-23-305-25-CPC-NH-B |
| Product name | Magnetic bar |
| Min. Fe-particle size that can be caught | 0,03 mm |
| Cleaning (ferrous particles disposal) method | Manual |
| Mounting interface | Pin with top cone |
| Material tube | AISI316L (SS 1.4404) |
| Surface treatment/finishing | S9: Polished, Ra 0,4 µm |
| Welds | WM: continuously welded |
| Max. operating temperature | 60 °C |
| Waterproof | Yes |
| Magnet quality | Neodymium N-42 |
| Flux density on magnet tube in contact with product (±10%) | 10700 gauss |
| Diameter | 23 mm |
| Length | 305 mm |
| Weight | 0,93 kg |