|  | Magnetic bar - heat resistant - N42SH Article number: SBANA100040-600 |
| --- | --- |

Attributes

| Description | Magnetic bar - heat resistant - N42SH |
| --- | --- |
| Article number | SBANA100040-600 |
| Product key | BAR-HT-23-600-25-2M8-NW-B |
| Min. Fe-particle size that can be caught | 0,03 mm |
| Cleaning (ferrous particles disposal) method | Manual |
| Mounting interface | Threaded hole M8 (2x) |
| Material tube | AISI316L (SS 1.4404) |
| Surface treatment/finishing | S9: Polished, Ra 0,4 µm |
| Welds | WM: continuously welded |
| Max. operating temperature | 140 °C |
| Waterproof | Yes |
| Magnet quality | Neodymium N-42SH |
| Flux density on magnet tube in contact with product (±10%) | 10700 gauss |
| Diameter | 23 mm |
| Length | 600 mm |
| Weight | 1,8 kg |