|  | Magnetic bar - extra powerful - N52 Article number: SBAQA100030-100 |
| --- | --- |

Attributes

| Description | Magnetic bar - extra powerful - N52 |
| --- | --- |
| Article number | SBAQA100030-100 |
| Product key | BAR-ES-23-100-25-1M8-NW-B |
| Min. Fe-particle size that can be caught | 0,03 mm |
| Cleaning (ferrous particles disposal) method | Manual |
| Mounting interface | Threaded hole M8 (1x) |
| Material tube | AISI316L (SS 1.4404) |
| Surface treatment/finishing | S9: Polished, Ra 0,4 µm |
| Welds | WM: continuously welded |
| Max. operating temperature | 60 °C |
| Waterproof | Yes |
| Magnet quality | Neodymium N-52 |
| Flux density on magnet tube in contact with product (±10%) | 11400 gauss |
| Diameter | 23 mm |
| Length | 100 mm |
| Weight | 0,31 kg |