|  | Pneumatic magnetic bar - N42-Ø34 mm - SECC400 Article number: SECC400916 |
| --- | --- |

Attributes

| Description | Pneumatic magnetic bar - N42-Ø34 mm - SECC400 |
| --- | --- |
| Article number | SECC400916 |
| Product key | SECC-S-400-N-MAGNET BAR D34 |
| Product name | Magnetic bar for SECC-240 |
| Min. Fe-particle size that can be caught | 0,03 mm |
| Cleaning (ferrous particles disposal) method | Automatic |
| Extra wear-resistant coating | No |
| Material | AISI304 (SS 1.4301) / AISI316L (SS 1.4404) |
| Max. operating temperature | 60 °C |
| Magnet quality | Neodymium N-42 |
| Flux density on magnet tube in contact with product (±10%) | 10000/8300 gauss |
| Diameter | 33,6 mm |
| Length | 1568 mm |
| Weight | 8,9 kg |