|  | Magnetic filter - industrial - manual cleaning - DN50 Article number: SSFI005038 |
| --- | --- |

Attributes

| Description | Magnetic filter - industrial - manual cleaning - DN50 |
| --- | --- |
| Article number | SSFI005038 |
| Product key | SFI-050-IF-05E-HT-F1m-S-B-B-B |
| Suitable for food production | For non-perishable foods only |
| Max. particle size | 10 mm |
| Min. Fe-particle size that can be caught | 0,03 mm |
| Production stop required during ferrous particles disposal | Yes |
| Cleaning (ferrous particles disposal) method | Manual |
| Ferrous particles disposal via | Manually taking out magnets + pulling them out of extractor |
| Build-in length | 230 mm |
| In-/outlet shape | Round |
| Interface connection type/size | DN50 acc. EN 1092-1 PN16 |
| Pressure drop (for water, at 1m/s) | 5 - 40 mbar |
| Magnet unit guidance for easy cleaning | No |
| Materials in contact with product | AISI316L (SS 1.4404) |
| Material seal between housing and door/magnet unit | Silicone VMQ, 70° Shore, EC1935/FDA, red |
| Surface finishing (interior/exterior) | S1: Grit blasted, Ra 3 µm |
| Welds inside the product channel | Wm: Continuously welded |
| Welds outside the product channel | Wm: Continuously welded where possible |
| Max. operating temperature | 140 °C |
| Min./max. ambient temperature | -10 to 60 °C |
| Max. operating pressure (pipeline pressure) | 10 bar |
| Test pressure | 15 bar |
| Magnetic system | Magnetic bar in extractor tube |
| Magnet quality | Neodymium N-42SH |
| Magnetic bars position / behaviour during production | Static, fixed position |
| Magnetic bar size | Extractor tube Ø25 mm; magnetic bar Ø23 mm |
| Number of magnetic bars | 5 |
| Flux density on (internal) magnetic bar (±10%) | 10700 gauss |
| Flux density on magnet tube in contact with product (±10%) | 8000 gauss |
| Sieve | No |
| Safety device between housing and door/magnet unit | No |
| Length | 230 mm |
| Width | 209 mm |
| Height | 220 mm |
| Weight | 15 kg |