|  | Inserto magnético - 5xN42SH-Ø23 mm - SFH-2,5" Número de artículo: E0020375 |
| --- | --- |

características

| Descripción | Inserto magnético - 5xN42SH-Ø23 mm - SFH-2,5" |
| --- | --- |
| Número de artículo | E0020375 |
| Clave del producto | SFH-S-2.5"-05E-HT INSERT |
| Product name | SFH-HT insert 2.5" |
| Suitable for food production | Yes |
| Max. particle size | 10 mm |
| Min. Fe-particle size that can be caught | 0,03 mm |
| Production stop required during ferrous particles disposal | Yes |
| Cleaning (ferrous particles disposal) method | Manual |
| Ferrous particles disposal via | Manually taking out magnets + pulling them out of extractor |
| Materials in contact with product | AISI316L (SS 1.4404) |
| Surface finishing (interior/exterior) | S5: Vibratory polished, Ra 0,4 µm, ex. welds and end faces |
| Welds inside the product channel | WM: Continuously welded |
| Welds outside the product channel | WM: Continuously welded |
| Max. operating temperature | 140 °C |
| Min./max. ambient temperature | -20 to 60 °C |
| Max. operating pressure (pipeline pressure) | 10 bar |
| Test pressure | 15 bar |
| Magnetic system | Magnetic bar in extractor tube |
| Magnet quality | Neodymium N-42SH |
| Magnetic bars position / behaviour during production | Static, fixed position |
| Magnetic bar size | Extractor tube Ø25 mm; magnetic bar Ø23 mm |
| Number of magnetic bars | 5 |
| Flux density on (internal) magnetic bar (±10%) | 10100 gauss |
| Flux density on magnet tube in contact with product (±10%) | 7600 gauss |
| Length | 130 mm |
| Width | 130 mm |
| Height | 139.5 mm |
| Weight | 3.3 kg |