|  | Filtro magnético - higiénico - barra simple - DN65 Número de artículo: E0117833 |
| --- | --- |

características

| Descripción | Filtro magnético - higiénico - barra simple - DN65 |
| --- | --- |
| Número de artículo | E0117833 |
| Clave del producto | SFH-065-T1-01M-HT-F5M-S-B-B-B |
| Suitable for food production | Yes |
| Max. particle size | 10 mm |
| Min. Fe-particle size that can be caught | 0,03 mm |
| Production stop required during ferrous particles disposal | Yes |
| Cleaning (ferrous particles disposal) method | Manual |
| Ferrous particles disposal via | Clean Out of Place (COP) |
| Build-in length | 200 mm |
| In-/outlet shape | Round |
| Interface connection type/size | Tube DN65 (Ø70x2 mm - acc. DIN 11850 R2/DIN 11866 A) |
| Pressure drop (for water, at 1m/s) | 5 - 40 mbar |
| Removable bottom for easier cleaning | Yes |
| Materials in contact with product | AISI316L (SS 1.4404) |
| Material seal between housing and door/magnet unit | Silicone VMQ, 70° Shore, EC1935/FDA, red |
| Surface finishing (interior/exterior) | S5: Vibratory polished, Ra 0,4 µm, ex. welds and end faces |
| Welds inside the product channel | WM: Continuously welded |
| Welds outside the product channel | WM: Continuously welded |
| Max. operating temperature | 140 °C |
| Min./max. ambient temperature | -20 to 60 °C |
| Max. operating pressure (pipeline pressure) | 10 bar |
| Test pressure | 15 bar |
| Magnetic system | Magnetic bar in tube |
| Magnet quality | Neodymium N-42SH |
| Magnetic bars position / behaviour during production | Static, fixed position |
| Magnetic bar size | Tube Ø65 mm |
| Number of magnetic bars | 1 |
| Flux density on magnet tube in contact with product (±10%) | 11300 gauss |
| Length | 200 mm |
| Width | 171 mm |
| Height | 329 mm |
| Weight | 11 kg |