|  | Extractor 5 staven - SFH-2" Artikelnummer: E0019442 |
| --- | --- |

Kenmerken

| Omschrijving | Extractor 5 staven - SFH-2" |
| --- | --- |
| Artikelnummer | E0019442 |
| Product key | SFH-S-2"-05E TOP EXTR |
| Type | Extractor for SFH-2 Neoflux® quick-cleaning hygienic magnet |
| Suitable for food production | Yes |
| Max. particle size | 16 mm |
| Materials in contact with product | AISI316L (SS 1.4404) |
| Surface finishing (interior/exterior) | S5: Vibratory polished, Ra 0,4 µm, ex. welds and end faces |
| Welds inside the product channel | WM: Continuously welded |
| Welds outside the product channel | WM: Continuously welded |
| Max. operating pressure (pipeline pressure) | 10 bar |
| Number of tubes | 5 |
| Tube diameter | 25 mm |
| Length | 90 mm |
| Width | 130 mm |
| Height | 130 mm |
| Weight | 1.6 kg |