|  | Deurafdichting silicone rood - SECFØ250 Artikelnummer: E0022626 |
| --- | --- |

Kenmerken

| Omschrijving | Deurafdichting silicone rood - SECFØ250 |
| --- | --- |
| Artikelnummer | E0022626 |
| Product key | SECF-S-250-SEAL SILI RED EC193 |
| Product name | Seal for Cleanflow magnet - Manual cleaning SECF-D250 |
| Suitable for food production | Yes |
| Material seal between housing and door/magnet unit | Silicone VMQ, 40° Shore, EC1935/FDA, red |