|  | Magneetrooster - Ø200 mm Artikelnummer: SEMR020078 |
| --- | --- |

Kenmerken

| Omschrijving | Magneetrooster - Ø200 mm |
| --- | --- |
| Artikelnummer | SEMR020078 |
| Product key | SMR-N-D200x50-JF-04E-S6-S |
| Product name | Magnetic grid |
| Shape | Round |
| Size | Ø200 mm |
| Max. particle size | 10 mm |
| Min. Fe-particle size that can be caught | 0,03 mm |
| Cleaning (ferrous particles disposal) method | Manual |
| Ferrous particles disposal via | Manually taking out magnets + pulling them out of extractor |
| Interface connection type/size | Jacob connection DN200 |
| Materials in contact with product | AISI316L (SS 1.4404) |
| Surface treatment/finishing | S1: Grit blasted, Ra 3 µm |
| Welds | WE: Intermittently welded |
| Extractor tubes brazed in housing | Yes |
| Max. operating temperature | 60 °C |
| Min./max. ambient temperature | -20 to 60 °C |
| ATEX marking | Free of own ignition sources |
| Suited for use in ATEX zone | 20, 21 and 22 |
| Waterproof | Yes |
| Magnetic system | Magnetic bar in extractor tube |
| Magnet quality | Neodymium N-42 |
| Magnetic bar size | Extractor tube Ø25 mm; magnetic bar Ø23 mm |
| Number of magnetic bars | 4 |
| Flux density on (internal) magnetic bar (±10%) | 10700 gauss |
| Flux density on magnet tube in contact with product (±10%) | 8000 gauss |
| Diameter | 215 mm |
| Height | 50 mm |
| Weight | 2,8 kg |