|  | Plaatmagneet - Ferriet - 500 mm Artikelnummer: SVMF050500 |
| --- | --- |

Kenmerken

| Omschrijving | Plaatmagneet - Ferriet - 500 mm |
| --- | --- |
| Artikelnummer | SVMF050500 |
| Product key | SVM-F-304x99-0500-B-F0E |
| Min. Fe-particle size that can be caught | 0,5 mm |
| Advised max. installation height | 90-140 mm |
| Production stop required during ferrous particles disposal | Yes |
| Cleaning (ferrous particles disposal) method | Manual |
| Ferrous particles disposal via | Manually by wiping |
| Installation/transport interface | Threaded hole M8 (6x) |
| Material housing | AISI304 (SS 1.4301) / S235JRC+C (St 1.0122) |
| Surface treatment/finishing | Painted |
| Welds | WE: Intermittently welded |
| Colour housing | Red (Traffic red): RAL3020 |
| Max. operating temperature | 100 °C |
| Min./max. ambient temperature | -20 to 60 °C |
| Magnetic system | Permanent ferrite magnet with flux boost |
| Magnet quality | Anisotropic ferrite F-33 |
| Magnet field strength (flux density) (±10%) | 2800 gauss |
| Length | 500 mm |
| Width | 304 mm |
| Height | 99 mm |
| Weight | 75 kg |