|  | Permanente blokmagneet - 951x343 mm Artikelnummer: SVMF081400 |
| --- | --- |

Kenmerken

| Omschrijving | Permanente blokmagneet - 951x343 mm |
| --- | --- |
| Artikelnummer | SVMF081400 |
| Product key | SVM-F-951x343-1460-B-F0E |
| Min. Fe-particle size that can be caught | 0,5 mm |
| Advised max. installation height | 155-440 mm |
| Production stop required during ferrous particles disposal | Yes |
| Cleaning (ferrous particles disposal) method | Manual |
| Ferrous particles disposal via | Manually by wiping |
| Installation/transport interface | Lifting eye Ø50 mm (4x) |
| Material housing | AISI304 (SS 1.4301) / S235JRG2 (St 1.0038) |
| Surface treatment/finishing | Painted |
| Colour housing | Blue (Ultramarine blue): RAL 5002 |
| Max. operating temperature | 100 °C |
| Min./max. ambient temperature | -20 to 40 °C |
| Magnetic system | Permanent ferrite magnet with flux boost |
| Magnet quality | Anisotropic ferrite F-33 |
| Magnet field strength (flux density) (±10%) | 2300 gauss |
| Length | 1465 mm |
| Width | 951 mm |
| Height | 433 mm |
| Weight | 1925 kg |