|  | Magneetrail - Ferriet - 102x24mm Artikelnummer: TBAB030003 |
| --- | --- |

Kenmerken

| Omschrijving | Magneetrail - Ferriet - 102x24mm |
| --- | --- |
| Artikelnummer | TBAB030003 |
| Product key | HRA-F-102x24-AB-0300-B-B |
| Shape/application | Straight |
| Weakening infeed | No |
| Weakening outfeed | Yes |
| Mounting interface | Threaded hole M8 (2x) |
| Material housing | AISI304 (SS 1.4301) / S235JRC+C (St 1.0122) |
| Surface treatment/finishing | Painted |
| Colour housing | Red (Traffic red): RAL3020 |
| Min./max. ambient temperature | -20 to 100 °C |
| Waterproof | No |
| Magnet type | Ferrite magnet, weakening outfeed |
| Magnet field strength (flux density) (±10%) | 1750 gauss |
| Length | 300 mm |
| Width | 102 mm |
| Height | 24 mm |
| Weight | 2,5 kg |