|  | Wirnik magnetyczny - 12xN45DH-Ø30 mm - SECR3030 Numer artykułu: E0006859 |
| --- | --- |

Właściwości

| Opis | Wirnik magnetyczny - 12xN45DH-Ø30 mm - SECR3030 |
| --- | --- |
| Numer artykułu | E0006859 |
| Klucz produktu | SECR-S-3030-12E-ES-B ROTOR |
| Product name | Rotor for Cleanflow rotating SECR-3030 |
| Suitable for food production | Yes |
| Max. particle size | 10 mm |
| Min. Fe-particle size that can be caught | 0,03 mm |
| Cleaning (ferrous particles disposal) method | Manual |
| Ferrous particles disposal via | Manually taking out magnets + pulling them out of extractor |
| Materials in contact with product | AISI316 (SS 1.4401) / AISI316L (SS 1.4404) |
| Surface finishing (interior/exterior) | S5: Vibratory polished, Ra 0,4 µm, ex. welds and end faces |
| Extra wear-resistant coating | No |
| Welds inside the product channel | Wm: Continuously welded |
| Welds outside the product channel | Wm: Continuously welded where possible |
| Max. operating temperature | 100 °C |
| Max. operating temperature in ATEX environment | 40 °C |
| Min./max. ambient temperature | -20 to 40 °C |
| Magnetic system | Magnetic bar in extractor tube |
| Magnet quality | Neodymium N-52 |
| Magnetic bars position / behaviour during production | Rotating, magnetic bars placed in a rotor |
| Magnetic bar size | Extractor tube Ø25 mm; magnetic bar Ø23 mm |
| Number of magnetic bars | 12 |
| Flux density on (internal) magnetic bar (±10%) | 13000 gauss |
| Flux density on magnet tube in contact with product (±10%) | 10500 gauss |
| Diameter | Ø205 mm |
| Length | 299 mm |
| Weight | 16 kg |